Araldite

Spectrum Report

Counts per second

Full scale: 14000 cps

Energy KeV

Full scale: 14000 cps

Counts per second

|  | Element | Counts per second |
| --- | --- | --- |
| C | Carbon | 1301 |
| O | Oxygen | 1320 |
| Al | Aluminum | 1151 |
| S | Sulphur | 13961 |

Energy KeV

Araldite 2

Counts per second

Full scale: 480 cps

Energy KeV

Full scale: 480 cps

Counts per second

|  | Element | Counts per second |
| --- | --- | --- |
| C | Carbon | 445 |
| O | Oxygen | 143 |
| Si | Silicon | 164 |

Energy KeV