Spectrum Report – All resins

Araldite

Counts per second

Full scale: 14000 cps

Energy KeV

Full scale: 14000 cps

Counts per second

|  | Element | Counts per second |
| --- | --- | --- |
| C | Carbon | 1301 |
| O | Oxygen | 1320 |
| Al | Aluminum | 1151 |
| S | Sulphur | 13961 |

Energy KeV

Araldite 2

Counts per second

Full scale: 480 cps

Energy KeV

Full scale: 480 cps

Counts per second

|  | Element | Counts per second |
| --- | --- | --- |
| C | Carbon | 445 |
| O | Oxygen | 143 |
| Si | Silicon | 164 |

Energy KeV

Araldite Slow

Counts per second

Full scale: 400 cps

Energy KeV

Full scale: 400 cps

Counts per second

|  | Element | Counts per second |
| --- | --- | --- |
| C | Carbon | 396 |
| O | Oxygen | 179 |
| Si | Silicon | 281 |

Energy KeV

Ciba Geigy

Counts per second

Full scale: 1600 cps

Energy KeV

Counts per second

|  | Element | Counts per second |
| --- | --- | --- |
| C | Carbon | 1498 |
| O | Oxygen | 672 |
| Cl | Chlorine | 1315 |

Full scale: 1600 cps

Energy KeV

EpoFix

Counts per second

Full scale: 5400 cps

Energy KeV

Counts per second

|  | Element | Counts per second |
| --- | --- | --- |
| C | Carbon | 4185 |
| O | Oxygen | 1772 |
| Cl | Chlorine | 1407 |

Full scale: 5400 cps

Energy KeV

EpoHeat

Counts per second

Full scale: 1200 cps

Energy KeV

Counts per second

|  | Element | Counts per second |
| --- | --- | --- |
| C | Carbon | 1154 |
| O | Oxygen | 108 |
| Cl | Chlorine | 559 |

Full scale: 1200 cps

Energy KeV

EpoThin

Counts per second

Full scale: 4800 cps

Energy KeV

Counts per second

|  | Element | Counts per second |
| --- | --- | --- |
| C | Carbon | 4722 |
| O | Oxygen | 2865 |
| Cl | Chlorine | 1039 |

Full scale: 4800 cps

Energy KeV

Epoxicure - 65°C Cure

Counts per second

Energy KeV

Full scale: 5400 cps

Full scale: 5400 cps

Counts per second

|  | Element | Counts per second |
| --- | --- | --- |
| C | Carbon | 5027 |
| O | Oxygen | 1888 |
| Cl | Chlorine | 820 |

Energy KeV

EpoxiCure - Room Temperature Cure

Counts per second

Full scale: 2800 cps

Energy KeV

Full scale: 2800 cps

Counts per second

|  | Element | Counts per second |
| --- | --- | --- |
| C | Carbon | 2433 |
| O | Oxygen | 1156 |
| Cl | Chlorine | 1185 |

Energy KeV

KonductoMet

Counts per second

Full scale: 2500 cps

Energy KeV

Counts per second

|  | Element | Counts per second |
| --- | --- | --- |
| C | Carbon | 2459 |
| O | Oxygen | 455 |

Energy KeV

Full scale: 2500 cps

Konductomet 2

Counts per second

Full scale: 16000 cps

Energy KeV

Full scale: 16000 cps

Counts per second

|  | Element | Counts per second |
| --- | --- | --- |
| C | Carbon | 4662 |
| O | Oxygen | 2927 |
| Al | Aluminum | 1074 |
| Si | Silicon | 14236 |

Energy KeV

Korapox 439

Counts per second

Energy KeV

Full scale: 5400 cps

Counts per second

Full scale: 5400 cps

|  | Element | Counts per second |
| --- | --- | --- |
| C | Carbon | 4882 |
| O | Oxygen | 1584 |
| Si | Silica | 613 |
| Cl | Chlorine | 1106 |

Energy KeV

Petropoxy

Counts per second

Full scale: 6400 cps

Energy KeV

Counts per second

|  | Element | Counts per second |
| --- | --- | --- |
| C | Carbon | 5443 |
| O | Oxygen | 2079 |
| F | Fluorine | 502 |
| Si | Silica | 498 |
| Cl | Chlorine | 351 |

Full scale: 6400 cps

Energy KeV

ProbeMet

Counts per second

Full scale: 3200 cps

Energy KeV

Counts per second

|  | Element | Counts per second |
| --- | --- | --- |
| C | Carbon | 420 |
| O | Oxygen | 234 |
| Al | Aluminium | 217 |
| Si | Silica | 2928 |

Energy KeV

Full scale: 3200 cps

ProbeMet 2

Counts per second

Full scale: 25000 cps

Energy KeV

Counts per second

|  | Element | Counts per second |
| --- | --- | --- |
| C | Carbon | 762 |
| O | Oxygen | 2631 |
| Cu | Copper | 23938 |
| Al | Aluminum | 1334 |
| Si | Silicon | 7509 |

Full scale: 25000 cps

Energy KeV

Robnor Resin

Counts per second

Full scale: 3600 cps

Energy KeV

Counts per second

|  | Element | Counts per second |
| --- | --- | --- |
| C | Carbon | 3473 |
| O | Oxygen | 12060 |
| Si | Silica | 513 |
| Cl | Chlorine | 1149 |

Full scale: 3600 cps

Energy KeV

Specifix

Counts per second

Full scale: 4200 cps

Energy KeV

Counts per second

|  | Element | Counts per second |
| --- | --- | --- |
| C | Carbon | 4526 |
| O | Oxygen | 1480 |
| Si | Silicon | 688 |
| s | Sulphur | 481 |
| Cl | Chlorine | 1530 |

Energy KeV

Full scale: 4200 cps

Transoptic

Counts per second

Full scale: 10000 cps

Energy KeV

Counts per second

|  | Element | Counts per second |
| --- | --- | --- |
| C | Carbon | 9925 |
| O | Oxygen | 1549 |
| Si | Silicon | 500 |

Full scale: 10000 cps

Energy KeV

TransOptic 2

Counts per second

Full scale: 280 cps

Energy KeV

Full scale: 280 cps

Counts per second

|  | Element | Counts per second |
| --- | --- | --- |
| C | Carbon | 279 |
| O | Oxygen | 258 |
| Na | Sodium | 43 |
| Cl | Chlorine | 168 |

Energy KeV

Varian

Counts per second

Full scale: 8000 cps

Energy KeV

Counts per second

|  | Element | Counts per second |
| --- | --- | --- |
| C | Carbon | 1428 |
| O | Oxygen | 2244 |
| Mg | Magnesium | 4632 |
| Si | Silicon | 7322 |
| S | Sulphur | 2042 |

Full scale: 8000 cps

Energy KeV

Varian 2

Counts per second

Full scale: 7200 cps

Energy KeV

Counts per second

|  | Element | Counts per second |
| --- | --- | --- |
| O | Oxygen | 1248 |
| Si | Silicon | 6574 |

Full scale: 7200 cps

Energy KeV